## Slide 1
Layer-by-Layer Defect Diagnostics in Two-Photon Polymerization Fusion Targets via Coherent Anti-Stokes Raman Scattering Microscopy
Zachary Schuder, Casey Frantz, Xi Huang1, Aofei Mao1, Peizi Li1, Sarah M. Fess2, Mark Bonino2, Dale Guy2, Dustin Floura2, David R. Harding2, and Yongfeng Lu1,*
Motivation and Challenges
Target Diagnostics
Spherical fuel capsule filled with deuterium-tritium (D-T) is struck by high-powered lasers from all sides to compress the capsule uniformly to extreme temperatures and pressures — triggering nuclear fusion.
Target quality is paramount: Microscale deviations in symmetry or material properties can lead to hydrodynamic instabilities during compression — leading to energy loss and preventing ignition.
Because fusion targets are so small and fragile, and because you only get one shot, it's crucial to analyze and qualify pre-implosion diagnostics of targets before use.
LASER ASSISTED
NANO ENGINEERING LAB (LANE)
1Department of Electrical and Computer Engineering, University of Nebraska-Lincoln (UNL), NE 68588
2University of Rochester-Laboratory for Laser Energetics (LLE), Rochester, NY 14623
*Email: ylu2@unl.edu
cryostat
CARS microscopy
D2-loaded targets at 12-20 K
Defect diagnosis
Distribution of fuel ice
3D CARS imaging and 3D reconstruction for target diagnosis
Surface scratches
r= 194.6 µm
θ= 4.1º
z= 48.8 µm
z
r
θ
r= 151.4 µm
θ= -28.7º
z= 758.4 µm
r= 197.2 µm
θ= -34.1º
z= 761.6 µm
3D survey of defects using GPS-like coordinates (r, θ, z)
Defect on the surface of outer shell wall
Defect inside the shell wall
Defect on the surface of inner shell wall
Cryo-CARS imaging of D2 ice at 12 K
3D reconstruction of D2 ice
CD shell
TPEF
CARS
D2 ice
Merged
Merged
Resolution < 1 µm
D2 ice cracks
D2 ice
Chart: IP-S
Two synchronized pulsed lasers (Pump beam + Stokes beam) Frequency difference matches molecular vibration
Coherently excites molecules, producing strong anti-Stokes signal
  Nonlinear process
  Signal only forms where beams overlap
Fast, 3D chemical imaging to identify voids, defects, and fuel layering.
Target Fabrication
Utilized two-photon polymerization to solidify liquid resin, building intricate geometries layer by layer.
Achieving superior uniformity is critical to enhance mechanical robustness, reduce defects, and improve overall target performance for high-yield fusion.
Excited
state
Ground
state
UV
Near-IR
3D Printing (TPP)
Final Product
Fs Laser
Resin (IP-S)
Substrate (ITO)
Focus on diagostics and defects
Move tpp section to bottom right
Fundamentals of CARS in bottom left
Experimental results in top right
Coherent Anti-Stokes Raman (CARS)
Challenges
ωpump
ωStokes
ωpump
ωanti-Stokes
ν0
ν1
Model (STL)
Up to
mm-sizes
Microscale pores
Nanoscale filaments
Foam target
This material is based upon work supported by the Department of Energy National Nuclear Security Administration University of Rochester “National Inertial Confinement Fusion Program” under Award Number DE-NA0004144.
Acknowledgment
Shell
Foam